1453444 CHL0010.1177/17475198261453444Journal of Chemical ResearchAbubakari et al.

research-article2026

Original Research Article

Journal of Chemical Research

| The effects of π-spacer on electronic properties, charge transfer, and chemical reactivity in D-A′-π-A configured molecules: | May-June 1–10 © The Author(s) 2026 Article reuse guidelines: sagepub.com/journals-permissions DOI: 10.1177/17475198261453444 journals.sagepub.com/home/chl |
| --- | --- |

Computational approach

Ismail Abubakari1, Michael Kennedy Sanama2

and Melkizedeck Hiiti Tsere3

Abstract

In this work, a systematic modification of the π-spacer was carried out to evaluate its influence on molecular geometry, 
electronic structure, charge transport properties, and global chemical reactivity descriptors in a series of D-A′-π-A 
organic molecules (M1–M4). Density functional theory was employed to analyze key parameters including dihedral angles, 
highest occupied molecular orbital–lowest unoccupied molecular orbital energies, natural bond orbital interactions, 
reorganization energies, ionization potential, electron affinity, chemical hardness, chemical potential, electronegativity, 
and electrophilicity index. The results reveal that M4 demonstrates the most favorable combination of properties, 
exhibiting the energy gap, reorganization energy, ionization potential, and chemical hardness of 1.4896, 0.4580, 4.8300, 
and 0.7127 eV, respectively. M4 also shows the highest chemical potential, electronegativity, and electrophilicity index 
of −4.1174, 4.1174, and 11.8938 eV, respectively. These results demonstrate the critical role of π-spacer engineering in 
adjusting the electronic behavior of D-A′-π-A systems and suggest that M4 is a promising candidate for high-performance 
organic semiconducting and optoelectronic uses.

Keywords 
DFT, D-A′-π-A, NBO, reorganization energy, global reactivity descriptors, charge transfer, HOMO-LUMO

Received: 15 January 2026; accepted: 6 May 2026

Introduction 	conjugation and ICT strength. Reorganization energies, for

| Organic | π-conjugated | donor-acceptor | systems | have | both holes (λhole) and electrons (λelectron), which describe the energetic cost associated with molecular relaxation during charge transfer, are equally important; lower reorganization |
| --- | --- | --- | --- | --- | --- |
| received considerable attention due to their broad applica-bility in nonlinear optics, organic electronics, and photo- |  |  |  |  |  |

voltaic technologies.1–4In these systems, the π-spacer that

connects donor and acceptor units is critical for modulating

intramolecular charge transfer (ICT), controlling molecular

1Department of Chemistry, College of Natural and Mathematical

planarity, and facilitating electronic coupling between sub-	Sciences, The University of Dodoma, United Republic of Tanzania

units.5–7Modifying the π-spacer, especially through the 	2Department of Chemistry, Muslim University of Morogoro, United

introduction of electron-donating or electron-withdrawing 	Republic of Tanzania

substituents, can significantly influence charge delocaliza-	3Department of Natural Sciences, College of Science and Technical 
	Education, Mbeya University of Science and Technology, United

tion, reorganization energies, molecular orbital distribu-

Republic of Tanzania

tions, and chemical reactivity descriptors.8–10 
	Natural bond orbital (NBO) analysis provides an effec-	Current affiliation: Michael Kennedy Sanama is also affiliated with 
		Department of Chemistry, College of Education, Dar es Salaam

tive method for examining charge distribution, donor-accep-

University, United Republic of Tanzania

tor interactions (via second-order perturbation theory), and 
electronic delocalization pathways.11Through evaluation of 	Corresponding author:

| stabilization energies between donor and acceptor orbitals, NBO analysis enables a quantitative understanding of how |  |  |  |  | Ismail Abubakari, Department of Chemistry, College of Natural and Mathematical Sciences, The University of Dodoma, Dodoma 41218, United Republic of Tanzania. Email: ismail.msangi2@udom.ac.tz |
| --- | --- | --- | --- | --- | --- |
| substituents | and | π-bridge | modifications | influence |  |

Creative Commons Non Commercial CC BY-NC: This article is distributed under the terms of the Creative Commons

Attribution-NonCommercial 4.0 License (https://creativecommons.org/licenses/by-nc/4.0/) which permits non-commercial use, 
reproduction and distribution of the work without further permission provided the original work is attributed as specified on the SAGE and 
Open Access pages (https://us.sagepub.com/en-us/nam/open-access-at-sage).

2 	Journal of Chemical Research

energies generally correspond to higher charge mobility and 	cyclopenta[b]thiophene. Any observed variations in elec-

improved electronic performance.8 	tronic or structural properties can be directly attributed to

In addition, global chemical reactivity descriptors, 	the influence of π-spacer, allowing a clear evaluation of its

including ionization potential, electron affinity, chemical 	effect on the D-A′-π-A molecular framework.

hardness, chemical potential, electronegativity, and electro-

| philicity, provide valuable insight into molecular stability and reactivity patterns. These descriptors, derived from | Computational details |
| --- | --- |

frontier molecular orbital (FMO) energies, help in estab-	The ground-state geometries of the molecules under investi-

| lishing | structure-property | relationships | in | D-A′-π-A | gation were taken from our earlier study,15where the |
| --- | --- | --- | --- | --- | --- |

chromophores and guide rational molecular design.11 	B3LYP16,17functional was used to fully optimize the molec-

Although several studies have used density functional 	ular structures using the Gaussian 09 Rev, D.01 program

theory (DFT) and time-dependent DFT (TD-DFT) to inves-	suite18within DFT. To guarantee structural stability, the

tigate the impact of π-bridges on D-π-A dyes (e.g. in dye-	M1–M4 structures were optimized using strict self-consist-

sensitized solar cells (DSSCs)),12fewer studies have 	ency field (SCF) convergence criteria. The geometries

comprehensively examined the combined effects of π-	match the verified minima discovered in our earlier study,15

spacer substitution on global descriptors, reorganization 	offering a consistent basis for the electronic analysis even

energies, and NBO interactions in D-A′-π-A molecular 	though formal frequency analyses were not carried out for

structures. Recent work has shown that incorporating vari-	this investigation. The optimized geometries described in

ous π-spacers into symmetrical non-fullerene acceptor 	that work form the structural basis of this study.

(A-D-A) systems can widen absorption ranges, lower reor-	This study focuses on a more thorough electronic inves-

ganization energies, and enhance photovoltaic perfor-	tigation of the developed sensitizers, building on this estab-

mance.13,14Similarly, benzothiadiazole-based π-spacers 	lished foundation. The Gaussian 09 Rev, D.01 program

have been reported to markedly influence band gaps, 	suite at the B3LYP/6-311G level of theory was employed

absorption strength, and charge-transport properties.8 	for all further computations. The B3LYP/6-311G level of

In this study, a series of D-A′-π-A molecules that differ 	theory was chosen in order to reconcile the systematic eval-

only in the π-spacer, with the donor, internal acceptor, and 	uation of the π-spacers with computing cost. Although it is

external acceptor held constant are developed. Using DFT 	accepted that the 6-311G basis set lacks polarization func-

at the B3LYP/6-311G level, the reorganization energies, 	tions, which are important for atoms like sulfur, and that

global chemical reactivity descriptors, and NBO character-	B3LYP may underrepresent long-range interactions, this

istics were evaluated. The analysis of π-spacer variations 	level of theory is suitable for capturing the qualitative-rela-

on charge delocalization, charge mobility, and molecular 	tive trends across the M1–M4 series. Therefore, rather than

reactivity offers insights to inform the development of 	being predictive-absolute numbers, the data reported here

advanced π-bridge-modified chromophores for optoelec-	are meant to offer a comparative understanding of the struc-

tronic applications. In addition, the photophysical proper-	tural influences on electronic properties.

ties and excited state arrangement of these developed 	The ionization potential (IP), the electron affinity (EA),

molecules, together with TD-DFT calculated absorption 	the energy of the highest occupied molecular orbital

maxima and oscillator strength, were established in our 	(HOMO) and the lowest unoccupied molecular orbital

previous work.15Building on those foundations, the current 	(LUMO), and the HOMO-LUMO energy gap are some of

work focuses on screening-level electronic and transport 	the important electronic parameters related to photovoltaic

descriptors to assess their feasibility for DSSC/organic 	performance that were computed based on the optimized

photovoltaic (OPV) uses. 	geometries. In addition, the reorganization energies for

hole and electron transfer (λhole and λelectron, respectively)

| Computational methodology | were determined, which reveals information about the mol- ecules’ charge-transport properties. |
| --- | --- |

| Molecular develop The π-spacer was selectively changed, maintaining the donor (D) unit, internal acceptor (A′), and external acceptor (A) constant across all molecular structures. The donor unit was chosen for its potent donating capacity, whereas benzo-thiadiazole (BTD) and cyanoacrylic acid were employed as the internal and external acceptors, respectively, to ensure efficient electron withdrawal. A series of four D-A′-π-A molecules (M1–M4), shown in Figure 1, was constructed by systematically varying the π-spacer. The selected π-spacers included thiophene, 4-(thiophene-3-yl)pyridine, 2-(4-(thiophene-2-yl)thiophene, and (E)-5,6-dihydro-6-(4,5-dihydrocyclopenta[b]thiophene-6-ylidene)-4H- | At the same theoretical level, NBO analysis was used to further clarify the ICT behavior inside the developed sensi- tizers. The FMO distributions were previously reported in our previous work,15but in order to provide the electronic context required for interpreting the newly evaluated ICT characteristics as well as charge-transport parameters of those developed molecules. Ground-state optimization was achieved using DFT/ 6-311G reliable with the methodology employed for the TD-DFT absorption analysis reported in our previous work.15Equations (1)–(4) were employed to determine the energy gap, reorganization energies for the electron (λelectron), reorganization energies for the hole (λhole), as well as total reorganization energy (λtotal)17,19,20 |
| --- | --- |

Abubakari et al. 	3

Figure 1. The D-A′-π-A molecules designed using donor, internal acceptor, π-spacer, and external acceptor.

| E | g | E LUMO | E HOMO | (1) | total | hole | electron | (4) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |

| hole | ( | E | 0 | E | ) | ( | E | 0 | E | 0 0 ) | (2) | where Eg indicates the energy band gap, EHOMO represents |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  | the HOMO energy, and ELUMO indicates the LUMO energy. |

The neutral, anion, and cation total energies in their respec-

| electron | E 0 | E | E | 0 | 0 E 0 | (3) | tive equilibrium structure are donated by E0 0 , E−−, and E+ +, |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | respectively; the cation/anion total energy in the neutral |

4 	Journal of Chemical Research

| geometry is E0 + / E0−and the neutral in the cation/anion | tures likely impact key properties, such as molecular polar- |
| --- | --- |

| geometry is E+ 0 / E−0 . | izability, charge transport behavior, and FMO alignment. |
| --- | --- |

Equations (5)–(10) were used to study various reactivity 	This pattern aligns with previous computational

parameters, including ionization potential (IP), electron 	research where, in twisted donor-acceptor systems, the

affinity (EA), chemical potential (μ), chemical hardness 	degree of orbital overlap and charge transfer character

(η), electronegativity (χ), and electrophilicity index (ω), 	were modulated by donor–acceptor dihedral angles.27

which provide information about the electrical structure of 	DFT analysis of aromatic systems connected to ethylene,

molecules21–24 	disilane, and ethynylene shows that a dihedral angle of

180° indicates ideal conjugation, while twisted geome-

| IPEHOMO | (5) | tries increase the HOMO-LUMO gap and decrease con- |
| --- | --- | --- |
|  |  | jugative interactions.28 |

| EAELUMO | (6) | Optoelectronic properties |
| --- | --- | --- |

The optoelectronic properties of the developed molecules

| (7) | as a function of π–spacer effect are here discussed using FMO energies (HOMO and LUMO energies) and the |
| --- | --- |

energy gap. Table 2 and Figure 3 display the HOMO

| ( | IP | EA1 | (8) | and LUMO energies (EHOMO and ELUMO) as well as the |
| --- | --- | --- | --- | --- |
|  |  | 2 |  | HOMO-LUMO energy gap (Eg) for D-A′-π-A proposed |

molecules (M1, M2, M3, and M4). Since EHOMO is fre-

| ( | IP | EA1 | (9) | quently linked to the molecule of interest’s capacity to |
| --- | --- | --- | --- | --- |
|  |  | 2 |  | donate electrons, larger EHOMO values signify a greater |

capacity to contribute electrons to a receptor’s vacant

2 	molecular orbital.15,29Conversely, a substance with a

| 2 | (10) | higher EHOMO can be regarded as an excellent electron |
| --- | --- | --- |
|  |  | carrier, but the molecule’s capacity to take electrons is |

correlated with its ELUMO value. As a result, a material

with a lower ELUMO value is more capable of accepting

Results and discussion 	electrons and acting as a carrier of holes.30

| Geometry optimization and dihedral angle | Smaller HOMO-LUMO gap values indicate increased conductivity and decreased kinetic stability.31M4 has the |
| --- | --- |

Although our earlier publication15established the structural 	smallest gap (1.4896 eV) among the series, suggesting a 
and FMO characteristics of the M1–M4 series, these param-	more robust intramolecular charge transfer character and 
eters are used here as a fundamental baseline to investigate 	a more efficient orbital coupling through the spacer. 
charge-transport dynamics that have not been explored 	Conjugation was not completely suppressed by the 
before. By adding NBO analysis and reorganization energy 	increased twist in M4, perhaps as a result of compensatory 
calculations, the current study greatly expands the current 	electrical effects. As observed in Figure 3, M3 is situated

| photophysical | profile | and | offers | deeper | mechanistic | between M1 and M2, with a very small gap (1.5830 eV). |
| --- | --- | --- | --- | --- | --- | --- |

insights into the electronic coupling and carrier mobility of 	Larger gaps (1.5919 and 1.6888 eV, respectively) are

these developed molecules. 	maintained by M1 and M2, which is consistent with either

Geometry optimization refers to the techniques used to 	significantly less conjugation or a more electron-with-

determine a molecule’s three-dimensional atomic arrange-	drawing character in the spacer. With the exception of

ment and reduce its model energy. Specific geometric vari-	steric effects or substituent interactions, the trend of

ables, such as the dihedral angle, were considered in order 	decreasing Eg, in the order M2 > M1 > M3 > M4, quali-

to assess the conformation of these proposed molecules. 	tatively coincides with increased conjugation and planarity

Figure 2 shows the optimal arrangement of each examined 	(lower twist). Greater ease of electrical excitation or charge

molecule. 	transfer is suggested by the narrower Eg in M4, which is

The dihedral angle between the donor, π-spacer, and 	advantageous in organic semiconductor or OPV settings;

acceptor units is a crucial factor in determining the degree 	however, stability and reorganization energy must also be

of planarity within the D-A′-π-A molecular architecture. 	balanced.

According to optimized geometries derived from DFT sim-	The M1–M4 series’ systematic π-spacer engineering is

ulations, molecule conformation is significantly influenced 	an atomic-scale molecular development technique intended

by the π-spacer’s nature. 	to adjust the degree of planarity and conjugation. This

Figure 2 and Table 1 show that the studied D-A′-π-A 	method successfully modifies the charge transfer character

molecules are planar, with dihedral angles near 180°. This 	and FMO (HOMO/LUMO) levels, which directly affects

indicates that the chosen π-spacers promote extended con-	the reorganization energies and the anticipated charge-

jugation throughout the donor-π-acceptor framework. Such 	transport and optoelectronic performance.32The study that

| planarity enables effective π-electron delocalization, which | follows | uses | these | electronic-structure | rationales | as |
| --- | --- | --- | --- | --- | --- | --- |

improves electrical communication between donor and 	screening-level descriptors to assess the dyes’ viability for

| acceptor units.25,26It is anticipated that these structural fea- | DSSC | applications, | building | upon | the | excited-state |
| --- | --- | --- | --- | --- | --- | --- |

Abubakari et al. 	5

Figure 2. The optimal structure for all proposed D-A′-π-A molecular systems.

profiles and TD-DFT absorption characteristics developed 	offers a helpful paradigm for examining intramolecular and

in our earlier work.15 	intermolecular linkages as well as bond interactions.33

Therefore, NBO analysis was carried out here to determine

| Charge population and Molecular linkage | the charge populations for the proposed molecules. Table 3 shows that the donor and π-linker groups of all the pro- |
| --- | --- |

When studying conjugative interactions or charge transfer 	posed molecules (except the π-linker in M2) possess posi-

in molecular systems, NBO analysis is a crucial tool. It 	tive NBO charges, confirming their effectiveness as

6 	Journal of Chemical Research

Table 1. The selected dihedral angle of the produced D-A′-π-A molecules.

| Molecules | D-A′ | A′-π | π-A |
| --- | --- | --- | --- |

| ANGLE | DEGREE | ANGLE | DEGREE | ANGLE | DEGREE |
| --- | --- | --- | --- | --- | --- |

| M1 | C12-C11-C23-C24 | –179.971 | C26-C28-C43-S42 | –179.950 | C40-C41-C32-C33 | 179.992 |
| --- | --- | --- | --- | --- | --- | --- |

| C10-C11-C23-C25 | –179.972 | C27-C28-C43-S39 | –179.960 |
| --- | --- | --- | --- |

| ]M2 | C12-C11-C23-C24 | 178.281 | C26-C28-C48-S47 | 175.023 | C40-C41-C44-C33 | 179.646 |
| --- | --- | --- | --- | --- | --- | --- |

| C10-C11-C23-C25 | 177.819 | C27-C28-C48-S49 | 174.821 |
| --- | --- | --- | --- |

| M3 | C12-C11-C23-C24 | –176.852 | C26-C28-C54-S53 | –175.527 | C48-C49-C32-C33 | 179.084 |
| --- | --- | --- | --- | --- | --- | --- |

| C10-C11-C23-C25 | –176.747 | C27-C28-C54-C50 | –175.997 |
| --- | --- | --- | --- |

| M4 | C12-C11-C23-C24 | –176.203 | C26-C28-C45-C44 | –175.590 | C49-C48-C32-C33 | 179.985 |
| --- | --- | --- | --- | --- | --- | --- |

Table 2. The EHOMO, ELUMO, and HOMO-LUMO energies gap 	Table 3. The NBO analysis for all proposed molecules M1–M4.

| for proposed M1–M4. | Molecules D | A′ | π | A | Δq(D-A) |
| --- | --- | --- | --- | --- | --- |

| Molecules | EHOMO (eV) | ELUMO (eV) | Egap (eV) | M1 | 1.11298 −1.2426 | 1.05896 −1.82755 | 2.94053 |
| --- | --- | --- | --- | --- | --- | --- | --- |

| M1 | –5.0540 | –3.4621 | 1.5919 | M2 | 1.12491 −1.24561 −1.06142 | 1.76896 −0.64405 |
| --- | --- | --- | --- | --- | --- | --- |

| M2 | –4.9786 | –3.2898 | 1.6888 | M3 | 1.09843 −1.24565 | 0.94466 −1.70516 | 2.80359 |
| --- | --- | --- | --- | --- | --- | --- | --- |

| M3 | –4.9163 | –3.3333 | 1.5830 | M4 | 1.10313 −1.24668 | 1.08663 −1.82643 | 2.92956 |
| --- | --- | --- | --- | --- | --- | --- | --- |

| M4 | –4.8469 | –3.3573 | 1.4896 |
| --- | --- | --- | --- |

The NBO charges on each dye molecule’s donor groups

|  | during photoexcitation were sorted as follows, based on Table 3; M2 (1.12491e) > M1 (1.11298e) > M4 (1.10313e) > M3 (1.09843e). M1 and M4 dominate in the donation capacity because M2 has a negative NBO value in its π-linker position that facilitates poor donation of electrons toward the acceptor. M1 and M4 can therefore give electrons more easily than the other molecules, based on these facts. The NBO charges for the acceptor groups were −1.82755, −1.76896, −1.70516, and −1.82643 for M1–M4, in that order. The electron donor and acceptor’s differential Δq(D-A) is also highlighted in the following order: M1 (2.94053e) > M4 (2.92956e) > M3 (2.80256e) > M2 (-0.64405e). Table 3 demonstrates that M1 and M4 have the largest Δq(D-A) of 2.94053e and 2.92956e. As a result, |
| --- | --- |

Figure 3. The electron excitation ability of the proposed 	M1 and M4 have a larger charge separation than other pro-

M1–M4 molecules. 	duced molecules. Therefore, it can be concluded that M4

outperforms M1 in charge separation. This is supported by

the comparison of their energy gaps and Δq(D-A) values,

electron-donating groups. Conversely, the negative NBO

where M4 exhibits a significantly larger reduction in energy

charges observed for both the internal and external acceptor

gap (0.1023 eV) and slightly higher Δq(D-A) with differ-

units (with the exception of the external acceptor in M2)

ence of 0.01097. So, these NBO metric contribute to the

indicate their strong electron-withdrawing ability.

hypothesis that an optimal π-spacer promotes better orbital

The negative charge concentrated on the M2 spacer

communication and charge separation, thereby improving

(−1.06142e) in the NBO analysis is a noteworthy finding

charge transfer characteristics.

that contract with positive charges found for the other spac-

Although ICT is essentially a dynamic excited-state

ers in this investigation. The M2 framework’s 4-(thiophene-

phenomenon, charge separation potential can be evaluated

3-yl)pyridine is responsible for this negative character

using ground-state NBO and FMO investigations as crucial

since it serves as an electron-accumulating site. From a

benchmarks. The strong spatial decoupling of FMOs in M1

kinetic standpoint, this concentrated negative density can

and M4 that were reported to our previous work,15where

be produced on electronic trap between the donor and the

the LUMO moves toward the anchoring group while the

anchoring group. In comparison to the other developed

HOMO stays localized on the donor, establishes a distinct

molecules, this design is anticipated to hinder the smooth

directional channel for electron migration.34The nearly

flow of electron density during excitation, which could

complete localization of orbitals on discrete donor-acceptor

slow down the injection kinetics and lower overall effi-

fragments affords a trustworthy approximation for the ICT

ciency of the charge transfer process.

Abubakari et al. 	7

Table 4. The electron, hole, and total reorganization energies 	Table 5. The global reactivity descriptors in (eV) for all

(in eV) for all proposed molecules (M1–M4). 	proposed molecules (M1–M4).

| Molecules | λelectron (eV) | λhole (eV) | λtotal (eV) | Molecules IP | EA | χ | η | µ | Ω |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

| M1 | 0.2209 | 0.1963 | 0.4172 | M1 | 5.0009 3.5293 4.2651 0.7358 −4.2651 12.3615 |
| --- | --- | --- | --- | --- | --- |

| M2 | 0.1595 | 0.2239 | 0.3834 | M2 | 4.8948 3.2398 4.0673 0.8275 −4.0673 | 9.9957 |
| --- | --- | --- | --- | --- | --- | --- |

| M3 | 0.2061 | 0.2147 | 0.4208 | M3 | 4.8646 3.3541 4.1093 0.7553 −4.1093 11.1794 |
| --- | --- | --- | --- | --- | --- |

| M4 | 0.2305 | 0.2275 | 0.4580 | M4 | 4.8300 3.4047 4.1174 0.7127 −4.1174 11.8938 |
| --- | --- | --- | --- | --- | --- |

mechanism, even if transition density matrix (TDM) analy-	trade-off between transport efficiency and light-harvest

sis offers a more detailed depiction of transition dynamics. 	capability determines a chromophore’s overall perfor-

This approach is in line with the body of research on push-	mance, even if lower reorganization energy is essentially

pull chromophores, confirming that the ground-state elec-	advantageous for transport kinetics. M4 is still a very com-

tronic topography effectively dictates the primary pathway 	petitive option due to its more optimized energy gap and

| for | charge | transfer | and | injection | kinetics | in | these | higher maximum absorption as reported to our previous |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |

systems.35 	paper,15even though M2 has better kinetic potential.

Therefore, rather than being distinguished by absolute

| Charge transfer | kinetic superiority over M2, M4 is classifies as a balanced architecture when advantageous charge mobility main- |
| --- | --- |

A key idea in comprehending charge transfer in organic 	tained within the 0.1-0.5 eV range complements its

molecules utilized in DSSCs and organic solar cells 	enhanced light-harvesting capabilities.

(OSCs) is reorganization energy. It stands for the energy

| required to react to an electron transfer event or a shift in the charge distribution within the molecule by rearranging | Chemical reactivity and electronic behavior |
| --- | --- |

the solvent, counterions, and neighboring molecules.36 	The electronic behavior and chemical reactivity of the con-

Molecules with lower reorganization energies are pre-	sidered molecules as a function of π-spacer is discussed

ferred for DSSCs and OSCs because they enable faster 	through its Global reactivity descriptors. The global reac-

charge transfer rates. Reorganization can be used to esti-	tivity descriptors provide complementary insights into the

mate the charge transfer characteristics of organic materi-	chemical reactivity and electronic behavior of the proposed

als, such as the speed at which electrons or holes can flow 	molecules. These parameters, derived from FMO energies,

within organic molecules.37 	help evaluate properties such as stability, charge transfer

The overall reorganization energies are calculated by 	propensity, and electrophilic/nucleophilic behavior. A high

adding the electron-reorganization and hole-reorganization 	energy bandgap indicates that the chemical system is more

energies. Equations 2−4 were used to compute these ener-	stable and less reactive.39Using HOMO and LUMO ener-

gies, and Table 4 displays the findings, where the total reor-	gies, we computed the ionization potential (IP), electron

ganization energies for all proposed molecules (M1–M4) 	affinity (EA), chemical potential (μ), electronegativity (χ),

are arranged in the order of M2 (0.3834 eV) < M1 (0.4172 	chemical hardness (η), and electrophilicity index (ω).

eV) < M3 (0.4208 eV) < M4 (0.4580 eV). The results 	Table 5 and Figure 4 show the results of global chemical

reveal that all developed molecules (M1–M4) exhibit lower 	descriptors for proposed molecules M1–M4.

reorganization energy. The observation that all the pro-	Electron affinity depicts the energy shift of a neutral

posed molecules exhibit relatively low reorganization ener-	molecule with the addition of an electron, whereas ioniza-

gies is consistent with the findings of Kacimi et al.,38who 	tion energy illustrates the energy change that results from

reported that dye molecules with total reorganization ener-	the removal of an electron from the molecule’s neutral

gies in the range of 0.1–0.5 eV tend to achieve higher 	state.40Understanding the ionization potential and electron

charge mobility. In this study, the calculated total reorgani-	affinity is necessary to solve fundamental issues in organic

zation energies fall within 0.3834–0.580 eV, supporting the 	chemistry, such as whether the molecules are more or less

assertion that these molecules possess favorably low reor-	reactive. For many organic substances, as well as the mol-

ganization energies. 	ecules under study, experimental measurements of ioniza-

The reduced reorganization energies observed in M1, 	tion energy and electron affinity are few. The energy barrier

M2, M3, and M4 can be attributed to the incorporation of 	for the injection of holes and electrons is directly related to

π-spacer units, which promote structural flexibility and effi-	the ionization potential and electron affinity. Higher elec-

cient intramolecular charge delocalization. Consequently, 	tron affinity values and a smaller ionization potential are

the low reorganization energies suggest that these dyes are 	desirable because they facilitate hole and electron injec-

capable of achieving higher electron-transfer efficiency. 	tion.41,42Table 5 and Figure 4 show the computed global

This property is expected to enhance electron mobility and, 	reactivity descriptors for the studied molecules. The fol-

ultimately, improve the overall electrical performance of the 	lowing is a ranking of the compounds according to their

proposed molecular systems. 	ionization potential: M4 < M3 < M2 < M1. The findings

When reorganization energies are compared, M2 has the 	indicate that M4 has the lowest ionization potential of all

lowest numerical value, suggesting an inherent kinetic 	the developed molecules, measuring 4.8300 eV. The mole-

advantage for charge transport. In material science, a 	cules are arranged according to electron affinity as follows:

8 	Journal of Chemical Research

Figure 4. The predicted reactivity of designed molecules using global reactivity descriptors.

M1 > M4 > M3 > M2, with M1 showing the highest val-	The electronegativity of an atom in a molecule is a

ues at 3.5293 eV. Due to its larger ionization potential dif-	measure of its capacity to attract electron density to itself.

ference (0.1709 eV) compared to the relatively small 	Among the numerous chemical characteristics that are

difference in electron affinity (0.1246 eV), M4 demon-	impacted by electronegativity are bond polarity, acidity,

strates superior hole- and electron-injection capability rela-	and basicity. Molecules that have a greater electronegative

tive to M1. 	value are more readily able to receive electrons. Table 5 and

In the ground state, the chemical hardness parameter 	Figure 4 rank the electronegativity values of the molecules 
describes the dye’s resistance to charge transfer and the ten-	as follows: M1 > M4 > M3 > M2. Based on the data pre-
dency of charge to escape from the system. This quality is 	sented in Table 5 and Figure 4, M1 and M4 exhibit the high-
essential to understanding the behavior of the chemical sys-	est electronegativity values among all the molecules. This

tem. The molecules are sorted as follows: M4 < M1 < M3 	indicates that these two systems have a stronger tendency

< M2. The calculated chemical hardness values are shown 	to attract and accept electrons compared to the others. 
in Table 5 and Figure 4. The results showed that the M4 		The electrophilic index is a helpful metric for assessing 
molecule had the lowest chemical hardness values. We get 	the electrophilic character of a molecule or a reaction site 
to the conclusion that M4 is more likely than the other mol-	within a molecule.21It provides details on a species’ elec-

ecules to release electrons and lower the barrier to ICT 	tron-taking propensity, which is crucial for understanding

because of the lower chemical hardness values. 	reaction mechanisms, determining reactivity, and develop-
	Chemical potential is sometimes known as the electronic 	ing new chemical processes. It was discovered that com-
chemical potential or the Fermi level. The energy required 	pounds with superior electrophilic groups have lower 
to add or remove an electron from the system at a constant 	chemical potential and decreased chemical hardness.44 
particle number and volume is a measure of the system’s 	Through the acquisition of electrons from the surrounding 
ability to donate or receive electrons. Chemical potential 	environment, a molecule with a higher electrophilicity 
has a major impact on both the electronic charge transfer 	index (ω) was shown to be more efficient and to have 
mechanism and the spontaneity of reactions. According to 	higher energy stability. Table 5 and Figure 4 display the 
Ayers, Anderson, and Bartolotti (2005), molecules with a 	electrophilicity index values, which are arranged as fol-
high electronic potential are good electron donors, whereas 	lows: M1 > M4 > M3 > M2. The results indicate that M1

those with a small electronic potential are good electron 	and M4 have higher electronegativity indices than the other 
acceptors.43Table 5 and Figure 4 display the computed 	molecules. Thus, it may be concluded that M1 and M4 pos-
chemical potential of the molecules in the following order: 	sess higher photoelectric properties.

M2 > M3 > M4 > M1. The results show that M2 has 		Actually, the global reactivity descriptors were computed 
higher chemical potential values, implying that it is effec-	at the B3LYP/6-311G theoretical level using Koopmans’the-
tive electron donor. This makes it easier for M2 to give 	orem. This functional is a well-known benchmark for organic 
electrons to the semiconductor, which acts as an electron 	photovoltaic materials, offering a balanced representation of 
acceptor. However, we make conclusion on that due to its 	the FMO, despite being sensitive to the 20% Hartree–Fock 
significant difference between M2 and M4 on energy gap 	exchange present in B3LYP. The relative trends in all descrip-
of 0.1992 eV while slight difference on chemical potential 	tors are thought to be reliable for forecasting the compara-

of -0.0501 eV so it makes M4 to be more favorable candi-	tive performance of these solar cell sensitizers because the

date to release electrons to the semiconductor rather than 	current work concentrates on the methodical comparison of

M2 based on these facts. 	structurally similar series (M1–M4).

Abubakari et al. 	9

Conclusion 	aspects and characterization techniques. Chem Soc Rev 2010;

39: 2577–2632.

Our computational analysis shows that the π-spacer’s type 	2. Wu W, Liu Y and Zhu D. π-Conjugated molecules with

has a major impact on the D-A′-π-A systems’ electrical 	fused rings for organic field-effect transistors: design, syn-

characteristics, charge transfer features, and chemical reac-	thesis and applications. Chem Soc Rev 2010; 39: 1489–1502.

tivity. With the lowest energy gap, reorganization energy, 	3. Oshi R, Abdalla S and Springborg M. Study of the influence

ionization potential, and chemical hardness of 1.4896, 	of functionalization on the reorganization energy of naphtha-

| 0.4580, 4.8300, and 0.7127 eV, respectively, among the molecules (M1–M4) under study, M4 stood out as the most viable candidate. These characteristics reflect enhanced charge transport capabilities and structural adaptability. In addition, M4 demonstrates the highest chemical potential, electronegativity, and electrophilicity index values of | lene using DFT. Comput Theor Chem 2017; 1099: 209–215. 4. Ersoy G and Henary M. Roadmap for designing donor-π-acceptor fluorophores in UV-Vis and NIR regions: synthesis, optical properties and applications. Biomolecules 2025; 15: 119. 5. Hasanein AA, Elmarassi YR and Kassem EN. TD-DFT investigation of D–π–A organic dyes with thiophene moie- |
| --- | --- |

−4.1174, 4.1174, and 11.8938 eV, respectively, indicating a 	ties as π-spacers for use as sensitizers in DSSCs. J Mol

strong tendency to accept electrons and participate in 	Model 2016; 22: 115.

favorable intermolecular interactions. The combined per-	6. Surendra Babu N, Kuot Malang MP and Abubakari I. DFT

formance metrics highlight M4 as a candidate for applica-	and TD-DFT Studies of D-π-A organic dye molecules with

tions in organic electronic and optoelectronic materials. 	different spacers for highly efficient reliable dye sensitized

| These insights may serve as a useful foundation for the rational design of advanced chromophores and semicon-ducting systems in future studies. | solar cells. Chemistryopen 2024; 13: 1–11. 7. Numbury SB, Khalfan MS and Vuai SAH. Theoretical studies of electronic and optical characteristics in donor-π- Acceptor (D-π-A) dyes: DFT and TD-DFT methods. Oxford |
| --- | --- |

| Acknowledgment | Open Mater Sci 2024; 4: 1–11. 8. Zaier R, Martel A and Antosiewicz TJ. Effect of benzothi­ |
| --- | --- |

The authors acknowledge the support of the Muslim University of 	adiazole-based π-spacers on fine-tuning of optoelectronic

Morogoro and the University of Dodoma. 	properties of oligothiophene-core donor materials for effi-

cient organic solar cells: a DFT study. J Phys Chem A 2023;

| ORCID iD | https://orcid.org/0009-0001-7674- | 127: 10555–10569. |
| --- | --- | --- |
|  |  | 9.Madrid-ÚsugaD,SuárezOJandPortacioA.Impactof |
| Michael Kennedy Sanama |  | molecular π-bridgemodificationsontriphenylamine-based |
| 6349 |  | donor materials for organic photovoltaic solar cells. Condens |

Matter 2025; 10: 1–12.

Ethical consideration 	10. Roy JK, Adhikari A and Lafferty T. Role of π-spacers and

In this article, there is no study employing animal or human subjects. 	acceptors in regulating the photophysical properties of BTPA 
	donor-based dyes: first-principles approach. J Phys Chem A

| Consent to participate | 2025; 129: 11104–11116. 11. Santaloci TJ, Meador WE, Wallace AM, et al. An automated |
| --- | --- |

Not applicable. 	quantum chemistry-driven, experimental characterization 
	for high PCE donor–p–acceptor NIR molecular dyes. Digit

Consent for publication 	Discov 2023; 2: 1269–1288.

| Not applicable. | 12. Vuai SAH, Khalfan MS and Babu NS. DFT and TD-DFT studies for optoelectronic properties of coumarin based |
| --- | --- |

| Author contributions | donor-π-acceptor (D-π-A) dyes: applications in dye-sensi- tized solar cells (DSSCS). Heliyon 2021; 7: e08339. |
| --- | --- |

Ismail Abubakari (Conceptualization), Michael Kennedy Sanama 	13. Zhu L, Zhang M, Zhong W, et al. Progress and prospects

(Writing original draft), and Melkizedeck Hiiti Tsere (Formal 	of the morphology of non-fullerene acceptor based high-

analysis). 	efficiency organic solar cells. Energy Environ Sci 2021; 1:

4341–4357.

Funding 	14. Rehman FU, Waqas M, Imran M, et al. Approach toward low

| The authors received no financial support for the research, author- ship, and/or publication of this article. | energy loss in symmetrical nonfullerene acceptor molecules inspired by insertion of different π-spacers for developing efficient organic slar cells. ACS Omega 2023; 8: 43792– |
| --- | --- |

| Declaration of conflicting interests | 43812. 15. Sanama MK, Abubakari I and Numbury SB. The effect of |
| --- | --- |

The authors declared no potential conflicts of interest with respect	π-spacer on D-A’-π-a system organic dyes for dye-sensitized

to the research, authorship, and/or publication of this article. 	solar cells (DSSCs) technology: a computational approach”.

Oxford Open Mater Sci 2024; 4: 1–9.

Data availability statement 	16. Becke AD. Density-functional thermochemistry. III. The

| Data supported by the article itself. | role of exact exchange. J Chem Phys 1993; 98: 5648–5652. 17. Lee C, Yang W and Parr RG. Development of the Colle- |
| --- | --- |

| References | Salvetti correlation-energy formula into a functional of the electron density. Phys Rev B 1988; 37: 785–789. |
| --- | --- |

1. Pron A, Gawrys P, Zagorska M, et al. Electroactive materi-	18. Frisch MJ, Trucks GW, Schlegel HB, et al. Gaussian 09,

als for organic electronics: preparation strategies, structural 	Revision D.01. R Soc Chem 2019; 1: 1–20.

10 	Journal of Chemical Research

19. Roy JK, Kar S and Leszczynski J. Electronic structure and 	properties of some semiconductors. Solid State Electron

optical properties of designed photo-efficient indoline-based 	1992; 35: 1343–1352.

dye sensitizers with D-A-Π-A framework. J Phys Chem C 	32. Zahra S and Kurban M. Sustainable design of green-func-

2019; 123: 3309–3320. 	tionalized π-conjugated BTBF-DPA derivatives for high-

20. Bourass M, Benjelloun AT, Benzoukar M, et al. DFT/ 	mobility hole transport. Tetrahedron 2025; 188: 134984.

TD-DFT characterization of conjugational electronic struc-	33. Rajan VK and Muraleedharan K. A computational investi-

tures and spectral properties of materials based on thieno [3, 	gation on the structure, global parameters and antioxidant

2-b][1] benzothiophene for organic photovoltaic and solar 	capacity of a polyphenol, Gallic acid. Food Chem 2017; 220:

cell applications. J Saudi Chem Soc 2017; 5: 563–574. 	93–99.

21. Islam N and Ghosh DC. On the electrophilic character of 	34. Mabkhot YN, Al-Showiman SS, Barakat A, et al. Compu­
	molecules through its relation with electronegativity and 		tational studies of 2-(4-oxo-3-phenylthiazolidin-2-ylidene) 
	chemical hardness. Int J Mol Sci 2012; 13: 2160–2175. 		malononitrile. BMC Chem 2019; 13: 11–11.

22. Parr RG and Pearson RG. Absolute hardness : companion 	35. Elhorri AM. Theoretical study of new push-pull molecules 
	parameter to absolute electronegativity. J Am Chem Soc 		based on transition metals for NLO applications and deter-
	1983; 105: 7512–7516. 		mination of ICT mechanisms by DFT calculations. J Theor 
23. Rocha M, Santo AD, Arias JM, et al. Ab-initio and DFT 		Comput Chem 2020; 19: 2050026.

calculations on molecular structure, NBO, HOMO–LUMO 	36. Hachi M, Slimi A, Benjelloun AT, et al. The influence 
study and a new vibrational analysis of 4-(Dimethylamino) 		of the structural variations in the π-bridge of D-π-A

benzaldehyde. Spectrochim Acta Part A Mol Biomol 	organic dyes on the efficiency of dye-sensitized solar 
	Spectrosc 2015; 136: 635–643. 	cells (DSSCs): a DFT computational study. In: 5th 
24. Wang H, Wang X, Wang H, et al. DFT study of new bipy-	International Conference on Renewable Energies for.

razole derivatives and their potential activity as corrosion 	Developing Countries, REDEC, Marrakech, Morocco,

inhibitors. J Ournal Mol Model 2007; 13: 147–153. 	29–30 June 2020, pp.1–6.

25. Li W, Wang J, Chen J, et al. Theoretical investigation and 	37. Babu NS and Riwa IO. DFT and TD-DFT studies of 1,3,5-

design of high-efficiency dithiafulvenyl-based sensitiz-	Tris (dipheny1amino) benzene derivatives based hole trans-

ers for dye-sensitized solar cells: the impacts of elongating 	port materials: application for perovskite solar cells. Opt

π-spacers and rigidifying dithiophene. Phys Chem Chem 	Quantum Electron 2022; 54: 1–16.

Phys 2014; 169458–9468. 	38. Kacimi R, Raftan M, Abram T, et al. Theoretical design of

26. Xie X, Liu ZH, Bai FQ, et al. Performance regulation of 	D-π-A system new dyes candidate for DSSC application.

thieno[3,2-b]benzothiophene π-spacer-based D-π-A organic 	Heliyon 2021; 7: e07171.

dyes for dye-sensitized solar cell applications: insights from 	39. Beheshtian J, Peyghan AA and Bagheri Z. Carbon nanotube

computational study. Front Chem 2019; 6: 676. 	functionalization with carboxylic derivatives: a DFT study.

27. Weissenseel S, Drigo NA, Kudriashova LG, et al. Getting 	J Mol Model 2013; 19: 391–396.

the right twist: influence of donor-acceptor dihedral angle on 	40. Li Y, Liu J, Liu D, et al. D-A-π-A based organic dyes for

exciton kinetics and singlet-triplet gap in deep blue thermally 	efficient DSSCs: a theoretical study on the role of π-spacer.

activated delayed fluorescence emitter. J Phys Chem C 2019; 	Comput Mater Sci 2019; 161: 163–176.

45: 27778–27784. 	41. Louis E and San-fabi E. Are electron affinity and ioniza-

28. Yamanoi Y. Theoretical comparison of ethylene-, disi-	tion potential intrinsic parameters to predict the electron or 
	lane- and ethynylene-bonded aromatic compounds from the 	hole acceptor character of amorphous molecular materials ? 
	viewpoint of conjugation formation. Phys Chem Chem Phys 	J Phys Chem Lett 2017; 8: 2445–2449.

2025; 27: 14517–14525. 	42. Heidari M, Janjanpour N, Vakili M, et al. Study of the ioni-
29. Sanama MK, Abubakari I and Babu NS. DFT and TD-DFT 		zation potential, electron affinity and HOMO-LUMO gaps 
	studies of the effect of internal acceptor based on D-A’-Π-A 		in the smal fullerene nanostructures. Chem Rev Lett 2018; 1:

structure for dye-sensitized solar cells. East African J Sci 	45–48.

Technol Innov 2024; 6: 1–17. 	43. Ayers PW, Anderson JSM and Bartolotti LJ. Perturbative

30. Abubakari I and Sanama MK. The effect of substituent 	perspectives on the chemical reaction prediction problem. 
	groups on D-A organic molecule system for organic solar 	Int J Quantum Chem 2005; 101: 520–534.

cells (OSCs) technology : A computational approach. Oxf 	44. Ayers PW and Parr RG. Variational principles for 
Open Mater Sci 2025; 5itaf004. 		describing chemical reactions: the Fukui function and

31. Ünlü H. A thermodynamic model for determining pressure 	chemical hardness revisited. J Am Chem Soc 2000; 122:

and temperature effects on the bandgap energies and other 	2010–2018.